

**FUTURE FOAM, INC.**

**PRODUCT DATA**

PRODUCT: FSTAT9000 PRODUCTION FACILITY: Newton, KS

DATE: June 2018

PHYSICAL PROPERTY VALUE UNITS TEST METHOD

Color: Pink visual

Density: 1.70-1.90 lbs. / cu.ft. ASTM D-3574-17

Indent. Force Deflection ASTM D-3574-17

@ 25% deflection: 81.0- 99.0 lbs. / 50 sq. in. (4” Specimen)

Static Decay: < 2.0 seconds FTMS 101C: Method 4046

Surface Resistivity: < 1011 ohms/square ASTM D257

Tensile Strength: > 10.0 p.s.i. ASTM D-3574-17

Elongation: > 100 % ASTM D-3574-17

Tear Resistance: > 0.8 lbs. / lin. inch ASTM D-3574-17

Compression Set ASTM D-3574-17

@ 50% comp.: < 12.0 %

An antistatic agent is added to our FutureStat® products during manufacturing which provides durable protection against static generation and build-up.

This foam product does not contain flame retardants as defined by California SB1019

\* Please see attached Polyurethane Foam Safety Bulletin

Corporate Lab

400 North 10th St. Council Bluffs, Iowa 51503

712-323-6718 800-733-8067 Fax 712-323-7163

www.futurefoam.com



**POLYURETHANE FOAM SAFETY BULLETIN**

November 2017

Flexible polyurethane foam, like all organic materials, will burn if exposed to a sufficient heat source. While the ignition temperature of flexible polyurethane foams may vary depending upon their chemical formulations, all polyurethane foams can burn and should be handled accordingly.

The potential risks from improper handling of flexible polyurethane foam are the risk of fire and resulting risks from toxic thermal decomposition products. Once ignited, polyurethane foams may melt to form combustible liquids, and will burn rapidly releasing great heat, consuming oxygen at a high rate, and generating dense smoke and toxic gases. In addition, gases released by the burning foam can be incapacitating or fatal if inhaled in sufficient quantities. In an enclosed space the resulting deficiency of oxygen will present a danger of suffocation to the occupants.

Any reference made with regard to any of our polyurethane products as being “Combustion Modified” is not to be construed as a guarantee, either express or implied , that these products will not burn and only indicates that a particular formulation has been tested under controlled laboratory conditions and meets or exceeds the requirements as set forth by a specific state or federal flammability standard. Furthermore, Future Foam, Inc. hereby only certifies that a particular formulation meets the requirements of a specific flammability standard on the day it is tested and does not guarantee that the same product will meet the requirements of the same test at any time in the future: Future Foam, Inc. does not make any guarantees, either expressed or implied, concerning the flammability characteristics of these products under actual fire conditions, and hereby specifically disclaims any liability incurred as a result of fire.

Corporate Lab

400 North 10th St. Council Bluffs, Iowa 51503

712-323-6718 800-733-8067 Fax 712-323-7163

[www.futurefoam.com](http://www.futurefoam.com)